Materials and Manufacturing 2 – List of Terms

Casting
Pouring liquid metal into a mould, having the shape of the product.

- Pattern		 replica of the desired product used for making the mould

- Flask			 support for the mould

- Cope 			 top part of the mould

- Drag 			 bottom part of the mould

- Parting line 		 seam between cope and drag

- Pouring basin		 molten metal is poured in

- Sprue			 metal flows downwards

- Running system 	 channels to transport the metal to the mould cavity

- Gates			 part of the running system

- Vents			 transport gases and hot air from the mould

- Risers			 supply additional metal to the casting as it shrinks during
 			    solidification

Lay-up
Placing layers of fiber-reinforced polymers onto a mould.

- Vacuum bagging film	 film to close the laminate from the outside

- Breather fabric	 ensures air can flow to the vacuum pump

- Bleeder fabric		 absorbs excess resin

- Peel ply		 ensures easy removal of other films after curing

Resin Transfer Moulding
Placing fibres into a closed mould, after which resin is sucked through it.

- Preform		 reinforcement shaped in shape of the mould

- Dry spots		 non impregnated areas after resin is added

- Pot life			 time until the resin viscosity starts to change

Filament Winding
Winding fibers (with resin on them) onto a rotating mould.

- Mandrel		mould for winding

- Reel			 holds the dry reinforcement fibers

- Winding angle		 angle under which the fibers are wound

- Geodescally		 reinforcement takes the shortest route from A to B

- Hoop winding		 winding under 90˚ angle

- Polar winding		 winding under 0˚ angle

- Helical winding	 winding under other angles

Forging
Shaping a work-piece by compressive forces.

- Slug			 workpiece (part of metal that is forged)

- Billet			 workpiece (part of metal that is forged)

- Preform		 workpiece (part of metal that is forged)

- Flash			 thin flat piece of metal attached to the product after forging

Metal / Polymer Extrusion & Pultrusion
Squeezing a metal/polymer through an opening with the shape of the final product.

- Billet			 ‘metal bar’

- Die			 opening that determines the shape of the product

- Profile			 the billet after it has passed the die

- Voids			 hollow section in a extrusion

- Rovings		 untwisted bundles of continuous filaments

Compression Moulding
Compressing a mix of reinforcement and resin between two mould-halves.

- Cavity			 bottom section of the mould

- Force / plug		 top section of the mould

- Moulding compound	 mix of reinforcement resin

- Charge			 mix of reinforcement resin

- Knitlines		 point where flow fronts merge, reinforcements can’t cross
 			    these lines

Deep Drawing
Using a punch to stamp a metal sheet into the desired shape.

- Metal blank		 flat piece of metal

- Blank holder		 clamp to ensure the blank doesn’t move

Separation by Shearing
Cutting a piece of material. (For example, by punching pieces out of a sheet.)

- Cutting blade		 blade to cut pieces of a material (Saw)

- Punching		 removing a part of the sheet by punching it.

- Blanking		 the same but now the part punched out is the product

- Nesting		 placing as many parts on a sheet as possible

- Beveling		 placing the punch under an angle to control the shear
 			    location

Separation by Removal
Separating a material by removing small pieces from it. (For example, sawing.)

- Kerf			 narrow zone that is removed from the workpiece.

- Chisel			 tool that removes chips from the workpiece

- Chips			 pieces removed from the workpiece

- Rake face		 side of the chisel on which the chip pushes

- Flank			 other side of the chisel